## Slide 1
DFM_RAMP_SUB-ASSY_MAGNET_BUD RET_L_B747_613-35106-90
Date: 2025/06/24
Rev.: 04

## Slide 2
B747 BUD | Revision list
Rev. | Description | Date
01 | Initial release | 2025/01/18
02 | Updated 2D drawing | 2025/01/18
03 | Optimize the fixture and hot press design, and change step 2 to use Shunt Carrier | 2025/05/09
04 | Update the automatic equipment | 2025/06/24

## Slide 3
B747 BUD | Product Information

## Slide 4
B747 BUD | Process Flow chart
Glue Dispensing
Loading Magnet
Glue cleaning
(Laser)
Hot Pressing
STEP-1
Unloading
Semi-Product
Glue Dispensing
Loading
Semi-Product
Shunt Loading
Hot Pressing
STEP-2
Unloading
Product
Glue Cleaning
Inspection
Packaging

## Slide 5
Glue cleaning & Unloading
1800
1500
MAG 4&3 Loading
1800
1600
MAG 2&1 Loading
Glue Dispensing
Hot Pressing
1500
1500
B747 BUD | Overview-STEP-1

## Slide 6
B747 BUD | Overview-STEP-2
1800
Hot Pressing
Semi-product loading
1800
1000
1400
Glue Dispensing
Shunt Loading
1500

## Slide 7
B747 BUD | STEP1- Loading Mag 1/2/3/4
Mag 4
Loading
Accurate
position
Polarity
detection
Polarity
detection
Accurate
position
Clamp 01
Tray 01
Tray 02
Clamp 02
Mag 3
Mag 4
Fixture Material : SKD 11
Mag 2
Mag 1
Mag 3
Loading
Mag 2
Loading
Mag 1
Loading
Magnets loaded

## Slide 8
Glue path detection
B747 BUD | STEP1- Glue Dispensing
Glue path diagram
(yellow area)
The Step1 Glue Dispensing Parameter |  | 
Glue | Type | HHD 8540
 | Storage | 2-8 ℃
 | Glue amount | 0.75 ± 0.15 mg (a product)
 | Glue position | As picture (a point in center)
 | Open time | < 60 S
Glue Dispensing | Type | MK-451 (SZ)
 | Mix nozzle elements | 16
 | Needle | 22 G

## Slide 9
B747 BUD | STEP1- Hot Pressing
Hot pressing chamber
X12
Robot
Prepressing
Side push
Pressing
Heating
Put the fixture into the hot pressing chamber
Take the fixture out of the hot pressing chamber
Air cylinder Type | TCM20X30S
Input air pressure | 0.4-0.6Mpa
Time | 80s
Temperature | 80±5℃

## Slide 10
B747 BUD | STEP1- Product glue cleaning and tray loading
Full Tray
with products
Return the empty fixtures
Incoming fixtures with products
Empty Tray
Laser device
Draw the product from the fixture
Glue cleaning by laser
Full tray with products
Glue cleaning parameters |  | 
Glue cleaning Machine | Name | Laser cleaning machine
 | Type | GM-C02-60-MR
 | Vendor | Guoyu
 | Rated power | 60 W
Parameters | Laser power | 42~54 W
 | Laser speed | 2500~4000 mm/s
 | Q frequency | 10~20 KHz
 | Fill the gap | 0.025~0.04 mm
Products in the fixture
Put the cleaned products into the tray

## Slide 11
B747 BUD | STEP2 – Semi-product loading
Shortage detection
Semi-product tray
Draw the smei-product from the tray
The Step-2 fixture design overview
Fixture base
Material:SUS304
Fixture Cover
Material: SUS304
18x fool-proofing magnets
Empty fixture
put the smei-product into the fixture
The smei-product loaded
Detect the shortage by Hall Coil

## Slide 12
B747 BUD | STEP2 - Glue Dispensing
The Step2 Glue Dispensing Parameter |  | 
Glue | Type | HHD 8540
 | Storage | 2-8 ℃
 | Glue amount | 1.10 ± 0.2 mg (a product)
 | Glue position | As picture (a point in center)
 | Open time | < 60 S
Glue Dispensing | Type | MK-451 (SZ)
 | Mix nozzle elements | 16
 | Needle | 22 G
Glue path diagram
(yellow area)
Glue path detection

## Slide 13
B747 BUD | STEP2 – Shunt loading
Shunt Suction Nozzle
Shunt Carrier design overview
Local view A
Local view B
V -CUT
V -CUT
Shunt Carrier
Shunt Carrier Disc
The shunt carrier disc conveys the shunt carrier
The shunt suction nozzle draws the shunt carrier
Put the shunt carrier on the product fixture
The shunt carrier attached on the product fixture

## Slide 14
B747 BUD | STEP2 – Hot Pressing
Input air pressure | 0.4-0.6 MPa
Time | 80s
Temperature | 80±5℃
Hot pressing chamber
Robot
Hot pressing
Put the fixture into the hot pressing chamber
Take the fixture out of the hot pressing chamber

## Slide 15
B747 BUD | STEP2 - Product Unloading
Remove the carrier waste
The products unloaded from the step2 fixture
Carrier waste
Carrier Location
Carrier Location
0.2Max
There is a gap at the edge after breaking
R0.15
There is a gap at the edge after breaking

## Slide 16
B747 BUD | Process Description - Glue Cleaning
Glue cleaning parameters |  | 
Glue cleaning Machine | Name | Laser cleaning machine
 | Type | GM-C02-60-MR
 | Vendor | Guoyu
 | Rated power | 60 W
Parameters | Laser power | 42~54 W
 | Laser speed | 2500~4000 mm/s
 | Q frequency | 10~20 KHz
 | Fill the gap | 0.025~0.04 mm
Automatic glue cleaning machine
Products loading tray
Products unloading tray
Robot
Glue cleaning station
Final Product
Laser device

## Slide 17
B747 BUD | Process Description - Inspection
Polar Pen
SST Tester
Flux Density Test
OMM Dimension Test

## Slide 18
B747 BUD | Process Description - Packaging
Place the products into tray
Qty:64Pcs
Qty:6 Layer*4 Tray/Layer* 64Pcs/Tray=1536pcs
Packing 4 trays with a wrapping film
Product 64x
Tray x1

## Slide 19
Thank you !