## Slide 1
DFM_RAMP_MAGNET_RADIAL_M2_MAGNETIZED_TE_B747_160-05690-90
Date: 2025/06/30
Rev.: 90

## Slide 2
B747 | Revision List
Rev. | Description | Date
01 | Initial Release | 2024/12/05
02 | Update 2D Drawing | 2025/03/04
03 | Update 2D Drawing | 2025/05/09
04 | Update 2D Drawing | 2025/06/20
90 | Page 17 has been updated to automatic magnetization & laser marking line | 2025/06/30

## Slide 3
B747 | Product Information

## Slide 4
B747 | Process Flow Chart
Block Magnet
1st Double Side Grinding
1st Wire Saw
2nd Wire Saw
1st Profile Grinding
3rd Wire Saw
Magnetizing
AOI Inspection
2nd Double Side Grinding
2nd Profile Grinding
Tumbling
Plating
Laser
Inspection
3rd Profile Grinding
Packaging

## Slide 5
B747 | Process Description _ Block
Block magnet with proper properties and dimension
Control Point:
Material Grade: N48SH-100RC(REE)
Br: 13.7-14.2kGs
Hcb: ≥ 13.2 kOe
Hcj: ≥ 19kOe
(BH)max: 45-49MGOe
Block magnet size: 57 × 43 × 35
Magnetic Properties Tester

## Slide 6
B747 | Process Description _ 1st Wire Saw
1st Wire Saw Parameter |  | 
Machine related | 型号 /Model | CX2121(CHT690)
 | 滚轮转速 /Wheel Speed | 800-1200m/min
 | 线径 /Wire Diameter | 0.25mm
 | 主进给速度 /Main Feeding Speed | 0.3-0.5mm/min
Process related | 料块摆放数量 /Block Qty | 2 × 3 × 4 × 2
 | 切片尺寸 /Slicing Dimension | 8.93±0.04 mm
 | 冷却液 /Coolant | DX-7A
Fixture related | L直角靠块 /Right-angle Block | 专用夹具 /Customized Made
 | 千分尺 /Micrometer | 0-25mm
 | 大理石底板 /Marble platform | 专用定制 /Custon Made
Material utilization ratio | 94% | 

## Slide 7
B747 | Process Description _ 1st Double Side Grinding
1st Double Side Grinding Parameter |  | 
Machine related | 型号/Model | M7625(M7635)
 | 砂轮材质/Wheel Material | 树脂砂轮 /Resin
 | 砂轮规格/Wheel SPEC | 250(350)x129x35
Process related | 研磨前尺寸/ Dimension Before Grinding | 8.93 × 43 × 35
 | 研磨后尺寸/ Dimension After Grinding | 8.809±0.02 × 43 × 35
 | 成型磨冷却液/ Coolant | ES232
Fixture related | 固定导槽/ Fixed Guide | 导轨 /Slideway
 | 千分尺/ Micrometer | 0-25mm
Material utilization ratio | 98.65% | 

## Slide 8
B747 | Process Description _ 2nd Wire Saw
2nd Wire Saw Parameter |  | 
Machine related | 型号/Model | DX2240(DX2260,CX680)
 | 滚轮转速/Wheel Speed | 800-1200m/min
 | 线径/Wire Diameter | 0.2mm
 | 主进给速度/Main Feeding Speed | 0.3-0.5mm/min
Process related | 料块摆放数量/ Block Qty | 6 × 8 × 5
 | 切片尺寸/ Slicing Dimension | 3.93±0.04 mm
 | 冷却液/ Coolant | DX-7A
Fixture related | L直角靠块/ Right-angle Block | 专用夹具 Custom Made
 | 千分尺/ Micrometer | 0-25mm
 | 大理石底板/Marble platform | 专用定制 Custon Made
Material utilization ratio | 91.4% | 

## Slide 9
B747 | Process Description _ 2nd Double Side Grinding
2nd Double Side Grinding Parameter |  | 
Machine related | 型号/Model | M7625(M7635)
 | 砂轮材质/Wheel Material | 树脂砂轮 /Resin
 | 砂轮规格/Wheel SPEC | 250(350)x129x35
Process related | 研磨前尺寸/ Dimension Before Grinding | 8.809 × 3.93 × 35
 | 研磨后尺寸/ Dimension After Grinding | 8.809 × 3.825±0.02 × 35
 | 成型磨冷却液/ Coolant | ES232
Fixture related | 固定导槽/ Fixed Guide | 导轨 /Slideway
 | 千分尺/ Micrometer | 0-25mm
Material utilization ratio | 97.33% | 

## Slide 10
1st Profile Grinding Parameter |  | 
Machine related | 型号 /Model | PG160
 | 砂轮材质 /Wheel Material | 金刚砂 /SiC
 | 砂轮规格 /Wheel SPEC | D160
Process related | 研磨前尺寸 /Dimension Before Grinding | 8.809 × 3.825 × 35
 | 研磨后尺寸 /Dimension After Grinding | 8.809 × (R21.5 / R24.5 x 3) × 35
 | 成型磨冷却液 /Coolant | ES232
Fixture related | 固定导槽 /Fixed Guide | 专用导轨 /Customized Slideway
 | 影像测试仪 /Image Tester | OMM
Material utilization ratio | 78.38% | 
B747 | Process Description _ 1st Profile Grinding

## Slide 11
B747 | Process Description _ 3rd Wire Saw
3rd Wire Saw Parameter |  | 
Machine related | 型号/Model | SDX1160MHR
 | 滚轮转速/Wheel Speed | 1000-1600m/min
 | 线径/Wire Diameter | 0.18mm
 | 主进给速度/Main Feeding Speed | 0.3-0.5mm/min
Process related | 料块摆放数量/ Block Qty | (1 × 10) × 8 ×4
 | 切片尺寸/ Slicing Dimension | 1.60±0.04 mm
 | 冷却液/ Coolant | GD260-A
Fixture related | L直角靠块/ Right-angle Block | 专用夹具 Custom Made
 | 千分尺/ Micrometer | 0-25mm
 | 大理石底板/Marble platform | 专用定制 Custon Made
Material utilization ratio | 88.18% | 

## Slide 12
B747 | Process Description _ 2nd Profile Grinding
2nd Grinding parameter |  | 
Machine related | 型号/Type | Grinding Machine With Two Grinding Wheels
 | 砂轮材质/Grinding Wheel Material | 金刚砂/Emery
 | 砂轮规格/Grinding Wheel Specification | D160
Process related | 研磨前尺寸/Dimension before Grinding | R24.5 x R21.5 x 3 x 8.81 x 1.60
 | 研磨后尺寸/Dimension after Grinding | R24.5 x R21.5 x 3 x 8.81 x Inner Arc
 | 成型磨冷却液/Coolant for Profile Grinding | M6
Fixture related | 固定导槽/Fixed Guide | 专用导轨/Customized Slideway
 | 影像测试仪/Image Measurement Instrument | OMM
Material utilization ratio | 74.05% | 

## Slide 13
B747 | Process Description _ 3rd Profile Grinding
3rd Grinding parameter |  | 
Machine related | 型号/Type | Grinding Machine With Two Grinding Wheels
 | 砂轮材质/Grinding Wheel Material | 金刚砂/Emery
 | 砂轮规格/Grinding Wheel Specification | D160
Process related | 研磨前尺寸/Dimension before Grinding | R24.5 x R21.5 x 3 x 8.81 x Inner Arc
 | 研磨后尺寸/Dimension after Grinding | R24.5 x R21.5 x 3 x 8.81 x Inner Arc / Outer Arc
 | 成型磨冷却液/Coolant for Profile Grinding | M6
Fixture related | 固定导槽/Fixed Guide | 专用导轨/Customized Slideway
 | 影像测试仪/Image Measurement Instrument | OMM
Material utilization ratio | 81.26% | 

## Slide 14
Remove the sharp edge of magnet
B747 | Process Description _ Tumbling
Tumbling Parameter |  | 
Machine related | 型号/Model | LZG200
 | 类型/Type | Vibrator
 | 容量/Volume | 200L
 | 转速（电压/频率)/speed | 45-50Hz
 | 振幅/Amplitude | -
Process related | 磨石VS磁钢配比 | 75±5 : 35±5
 | 装载量（容量L）/Loadage | 35±5kg
 | 振磨时间/Time | 10~12 hrs
 | 磨石规格/size | Φ16圆球 & 18*18斜三角
 | 磨石材质/Material | SiC
Fixture related | 过滤网/Filter screen | -

## Slide 15
B747 | Process Description _ Plating (CU+EN Plating)
Plating Process Flow Chart
Ultrasonic degreasing
Activation
Acid pickling
Copper plating
Activation
EN plating
Main Process:
Copper plating
1. Plating layer thickness
Cu: 2.5-5 μm
2. Qty.: 4~5kg /1barrel /70-90min
1. Plating layer thickness
EN: 2-4 μm
2. Qty.: Qty.:4~5kg /1barrel /70-90min
EN plating

## Slide 16
B747| Process Description _ AOI Inspection
AOI Inspection

## Slide 17
1600mm
1400mm
1000mm
1800mm
B747| Process Description _ Magnetizing/ Laser Marking
Flex Vibration Feeder Module
Magnetizing module
Flexible Vibrating Plate
Contoured Nozzle
Magnetizing coils
Laser Marking & Unloading Module
Laser Marking Parameter |  | 
Machine related | Type/型号 | GM-F-D-XT-20
 | Output/输出功率 | 20W
 | Frequency/频率 | 80KHZ
Processing related | Speed/速度 | 800-1300mm/s
 | Q Frequency/Q频率 | 45-60KHz
 | Jump Speed/空跳速度 | 3000mm/s
 | Power%/使用功率% | 25-45%
 | Filling Spacing/填充间距 | 0.025-0.05mm
Magnetizing Parameter | 
Magnetizing machine Type | KCJ-35M
Magnetizing coil Type | TCG-S
Magnetizing coil Size | 110*75*150 mm
Magnetizing Voltage | 3000 V
Magnetizing Capacitance | 9000μF
Automated Equipment Flow chart
(Picture for reference only)
Automated Magnetizing & Laser Marking Line
Loading Magnet
Magnetizing
Laser Marking
Load the Magnet into the tray

## Slide 18
B747| Process Description _ Inspection Device
SST Test
XRF Coating Test
Polar Pen
Fluxmeter+ Helmholtz coil
OMM Dimension test
Flux density Test

## Slide 19
B747 | Process Description _ Packaging
Place the products into tray
Qty: 64 Pcs
Qty:64 Pcs/Tray * 30 Tray =1920pcs
Put 5 trays into a Vacuum bag
64*Products
1*Packaging Tray

## Slide 20
Thank you !